ILLINOIS VALLEY COMMUNITY COLLEGE

## COURSE OUTLINE

DIVISION:

COURSE:  	WLT 1230  AWS Testing:   Dual Shield and                              Metal Core

Date:       Fall  2012

Credit Hours: 	2

Instructor: Paul Leadingham

Phone: 815-224-0319

Email: Paul_Leadingham@ivcc.edu

Prerequisite(s):	None

Delivery Method:  	 Lecture	  Contact Hours (1 contact = 1 credit hour)

Seminar 	   Contact Hours (1 contact = 1 credit hour)

Lab  	   Contact Hours (2 contact = 1 credit hour)

Clinical  	   Contact Hours (3 contact = 1 credit hour)

Online

Blended

Offered:   Fall       Spring       Summer

IAI Equivalent –Only for Transfer Courses-go to http://www.itransfer.org:

CATALOG DESCRIPTION:

In this course, theory and practice in the preparation and welding of all position mild  steel plate joints, using Dual Shield and Metal core will be explored. Safety, equipment components, nozzle set-up, travel direction, torch angles, weave and stringer techniques will be taught. Joints that are prepared and welded in accordance with the American Welding Society (from hereon known as AWS), standards used in industry and construction will be stressed.. All position welds are accomplished on the appropriate plate and practice tests will be given according to AWS criteria. The student will practice and prepare for the AWS Certification Test in the Flat position.   Lecture, one hour a week; Lab, two hours a week.

GENERAL EDUCATION GOALS ADDRESSED

[See the last page of this form for more information.]

### Upon completion of the course, the student will be able:

### [Choose those goals that apply to this course.]

To apply analytical and problem solving skills to personal, social and

professional issues and situations.

To communicate orally and in writing, socially and interpersonally.

To develop an awareness of the contributions made to civilization by

the diverse cultures of the world.

To understand and use contemporary technology effectively and to

understand its impact on the individual and society.

To work and study effectively both individually and in collaboration with

others.

To understand what it means to act ethically and responsibly as an

individual in one’s career and as a member of society.

To develop and maintain a healthy lifestyle physically, mentally, and

spiritually.

To appreciate the ongoing values of learning, self-improvement, and

career planning.

EXPECTED LEARNING OUTCOMES AND RELATED COMPETENCIES:

### [Outcomes related to course specific goals.]

Upon completion of the course, the student will be able to:

The following objectives will be completed in the welding lab in all positions. The student will be able to:

1.	Understand and demonstrate safe work practices in the welding shop in regards to working with the Gas Metal Arc Welding equipment using Dual Shield and Metal Core wires.

2.	Demonstrate an ability to cut and prepare plate coupons.

3.	Demonstrate an ability to properly align and tack plate coupon assemblies.

4.	Demonstrate an ability to correctly position and weld out the plate coupon assemblies in all positions, to conform to Standard Welding Procedure Specifications by the AWS. Also, Demonstrate an ability to do this position welding on 1" thick mild steel to prepare for the certifaction test.

5.	Demonstrate an ability to conduct a Visual Examination Inspection of these welds according to AWS criteria.

6.	Be able to complete an AWS Certified Welder Application properly.

7.	Demonstrate an ability to prepare, stamp ID letters and numbers and tack weld into position, AWS certified test coupons (1" X6" mild steel), in the flat position.

8.	Demonstrate an ability to read and correctly follow the WPS.

9.	Demonstrate an ability to correctly weld out the test.

10.    Demonstrate an ability to mark, cut out and properly grind the test specimens from the welded test. Then, observe the CWI tester bend the test specimens and explain the results to the student.

COURSE TOPICS AND CONTENT REQUIREMENTS:

Shop Safety, Types of weld joints, Proper handling procedures of plate before and after welding, Visual inspection and AWS destructive testing.

INSTRUCTIONAL METHODS:

Classroom lecture and weld lab hands-on instruction.

INSTRUCTIONAL MATERIALS:

Video’s, selected hand-out sheets, welded examples, welding textbook and workbook.

STUDENT REQUIREMENTS AND METHODS OF EVALUATION:

Students would be required to furnish all proper protective equipment to safely perform in the welding lab environment. A Modern Welding Textbook and Workbook (by G-W publishers) would also be required.  Student progress will be charted on the instructor’s evaluation matrix chart which will include areas like project performed, date completed, grade and any specific notes that may relate to the students progress.

OTHER REFERENCES

Lincoln Electric Welding Technology Center

Hobart Institute of Welding Technology

American Welding Society.

This workforce solution was funded by a grant awarded by the U.S. Department of Labor’s Employment and Training Administration. The solution was created by the grantee and does not necessarily reflect the official position of the U.S. Department of Labor. The Department of Labor makes no guarantees, warranties, or assurances of any kind, express or implied, with respect to such information, including any information on linked sites and including, but not limited to, accuracy of the information or its completeness, timelines, usefulness, adequacy, continued availability, or ownership. This solution is copyrighted by the institution that created it. Internal use, by an organization and/or personal use by an individual for  non-commercial purposes, is permissible. All other uses require the prior authorization of the copyright holder.

Course Competency/Assessment Methods Matrix

| WLT 1230 AWS Testing: Dual Shield and Metal Core | Assessment Options |
| --- | --- |
| For each competency/outcome place an “X” below the method of assessment to be used. | Assessment of Student Learning | Article Review | Case Studies | Group Projects | Lab Work | Oral Presentations | Pre-Post Tests | Quizzes | Written Exams | Artifact Self Reflection of Growth | Capstone Projects | Comprehensive Written Exit Exam | Course Embedded Questions | Multi-Media Projects | Observation | Writing Samples | Portfolio Evaluation | Real World Projects | Reflective Journals | Applied Application (skills) Test | Oral Exit Interviews | Accreditation Reviews/Reports | Advisory Council Feedback | Employer Surveys | Graduate Surveys | Internship/Practicum /Site Supervisor Evaluation | Licensing Exam | In Class Feedback | Simulation | Interview | Written Report | Assignment |
| Assessment Measures – Are direct or indirect as indicated. List competencies/outcomes below. | Direct/ Indirect | D | D | D | D | D | D | D | D | D | D | D | D | D | D | D | D | D | D | D | I | I | I | I | D | D |  |  |  |  |  |  |
| 1. Understand and demonstrate safe work practices in the welding shop in regards to working with the Gas Metal Arc Welding equipment using Dual Shield and Metal Core wires. |  |  |  |  | X |  |  |  | X |  |  |  |  |  | X |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2. Demonstrate an ability to cut and prepare plate coupons. |  |  |  |  | X |  |  |  | X |  |  |  |  |  | X |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3. Demonstrate an ability to properly align and tack plate coupon assemblies. |  |  |  |  | X |  |  |  | X |  |  |  |  |  | X |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4. Demonstrate an ability to correctly position and weld out the plate coupon assemblies in all positions, to conform to Standard Welding Procedure Specifications by the AWS. Also, Demonstrate an ability to do this position welding on 1" thick mild steel to prepare for the certifaction test. |  |  |  |  | X |  |  |  | X |  |  |  |  |  | X |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5. Demonstrate an ability to conduct a Visual Examination Inspection of these welds according to AWS criteria. |  |  |  |  | X |  |  |  | X |  |  |  |  |  | X |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6. Be able to complete an AWS Certified Welder Application properly. |  |  |  |  |  | X |  |  |  |  |  |  |  |  | X | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7. Demonstrate an ability to prepare, stamp ID letters and numbers and tack weld into position, AWS certified test coupons (1" X6" mild steel), in the flat position. |  |  |  |  | X |  |  |  |  |  |  |  |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8. Demonstrate an ability to read and correctly follow the WPS. |  |  |  |  | X |  |  |  |  |  |  |  |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9. Demonstrate an ability to correctly weld out the test. |  |  |  |  | X |  |  |  |  |  |  |  |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 10. Demonstrate an ability to mark, cut out and properly grind the test specimens from the welded test. Then, observe the CWI tester bend the test specimens and explain the results to the student. |  |  |  |  | X |  |  |  |  |  |  |  |  |  | X |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |