KISHWAUKEE COLLEGE SYLLABUS

Spring 2014

Shielded Metal Arc Welding II 2 Credit Hours WT124 -5BO1 Tuesday, Thursday 3:30-6:15pm RM A1430 &A1431

03/18/2014-05/16/2014

Bernard Hackler

Room A1429

Office hours :M 8:30-10am, T 2-3:30pm,W8:30-10am, Th 2-3:30pm

Office phone: 815-825-2086 x 6151

Office hour by appointment

Instructor Kishwaukee College email Bernard.Hackler@kishwaukeecollege.edu

COURSE DESCRIPTION

Prerequisite:   WT 122

A continuation of theory and practice in Shielded Metal Arc Welding (SMAW). Single and multi-pass V-grooves with and without backing in all four positions are emphasized.  Introduction of non-destructive inspection as well as application of destructive testing through guided bend tests is included.

One hour lecture/discussion and two hours lab a week.

STUDENT LEARNING OUTCOMES

- Develop and practice safe work habits.

- Identify and correctly adjust amperage for various sizes and types of electrodes per material thickness.

- Demonstrate proficiency in groove weld processes, including V-grooves with and without backing.

- Weld low carbon steel in the flat, horizontal, vertical, and overhead positions on grooves.

- Develop a basic understanding of welding codes, standards, procedures and

qualifications as applicable to groove welds.

6.   Apply visual and non-destructive practices for testing and inspection of weld joints.

7.   Appraise weld quality using the guided bend test procedure.

TEXT(S) Welding Principles and Applications – Seventh Edition; Larry Jeffus

ISBN:  978-1-111-03917-2

REQUIRED STUDENT MATERIALS

1.	Long cotton pants with no holes

2.	Long sleeved cotton shirt or welding coat-Flame Retardant

3.	Leather shoes

4.	Safety glasses ANSI Z87.1

5.	Welding hood with a #10 lens for SMAW

6.	Diagonal cutting pliers/MIG pliers

7.	Welding gloves

8.	8 inch adjustable pliers (channel-locks)

9.	Wire brush

10.	Welder’s chipping hammer

11. 	Welder’s cap

For the safety of all students, instructor reserves the right to determine if these requirements have been met.

ADDITIONAL STUDENT REFERENCES AND THEIR LOCATION (if applicable )

None

BREAKDOWN OF COURSE REQUIREMENTS

Exams……………................20%

Participation............………...10%

Homework………………….10%

Weld Coupons……………...60%

FINAL GRADE DETERMINATION

90 - l00   = A

80 - 89    = B

70 - 79    = C

60 - 69    = D

59 - below = F

Grade reports will not be mailed out.  Please check KishSOS, My Student Info, under Academic

Profile, Grades, for grade reports.

COURSE EXIT REQUIREMENTS (if applicable) Click here to enter text.

MAKE-UP POLICY (for tests and other course requirements) Make-up tests and other course requirements must be prearranged with instructor.

ATTENDANCE POLICY

If you miss 3 days or more and do not make them up, there will be a 35% reduction in your grade

CLASS WITHDRAWAL

A “W” cannot be given as a final grade.  The student is responsible for officially withdrawing from the class according to procedures described in the college catalog.  Any student that does not officially withdraw from the class will receive a letter grade.  The last date for withdrawal for this course can be found at “My Class Schedule” on KishSOS.  Kishwaukee College reserves the right to administratively withdraw at midterm those students who are not actively pursuing course objectives or who are in violation of standards of behavior as outlined in the Student Code of Conduct and Discipline.  For a copy of the student conduct policy, contact the Vice President of Student Services Office or refer to the Kishwaukee College catalog.

INCOMPLETE GRADE

All course requirements must be completed by the end date for the course. In the event that extremely difficult circumstances merit granting a student more time to finish course requirements, an “Incomplete” (I) grade may be given.  Taking an Incomplete is possible only at the instructor's discretion.  To receive an Incomplete, a contract between the student and the instructor must be completed and approved regarding the completion of all remaining work within a strictly defined period of time.  If the conditions of the contract are not met, an “I” grade may revert to an “F”.

CLASS CANCELLATIONS

Class cancellations due to inclement weather will be posted on the College Website: www.kishwaukeecollege.edu. or announced by the local radio stations.  Students may also call the College at (815) 825-2086. Class cancellations due to instructor absence will be posted on the classroom door and posted at www.kishwaukeecollege.edu/class_cancellations. Room changes will be announced in advance whenever possible and posted on the classroom door.

ACADEMIC DISHONESTY

In order to evaluate student work, faculty must be able to trust that the work is original with a student and not the work of someone else. Cheating, falsifying information, forgery, plagiarism, and other dishonest actions will not be tolerated. Sanctions for academic dishonesty are at the discretion of the instructor and subject to appeal as provided in Student Code of Conduct and Discipline. A complete explanation of the policy and procedures surrounding academic dishonesty are outlined in the Kishwaukee College Catalog.

COPYRIGHT

As a Kishwaukee College Student, you may have copyrighted materials or software made available to you by the college for course use.  Please understand that copyright law may prohibit copying these materials.  Violation of copyright laws can lead to prosecution for a criminal offense. You are required to abide by the specific copyright and licensing agreements that apply to each particular piece of software.

GRADUATION REQUIREMENTS FOR TRANSFER DEGREE STUDENTS

All students intending to graduate with an A.A., A.S., A.E.S., or A.F.A. are required to submit a complete Degree Portfolio.  The Degree Portfolio is a means for the institution to measure its effectiveness in preparing students for successful completion of a degree at a transferring institution.  Save your college-level work throughout your academic career in order to facilitate the portfolio compilation.  Also, submit a completed application for graduation from the college the semester that you plan on graduating prior to submitting the complete Degree Portfolio.  Guidelines and the specific requirements (along with the rubrics used for assessment) for the Degree Portfolio can be found at www.kishwaukeecollege.edu/portfolio.

ASSISTIVE RESOURCES CENTER/DISABILITY SERVICES

Any student with a documented disability or special learning need and wanting to request accommodations, should contact the Coordinator in A1317 or at (815) 825-2086 ext 3960, (815) 825-9106 (TTY), or send an email to awilson@kishwaukeecollege.edu. The student’s disability must impact their ability to participate in the educational environment and be documented by an appropriate professional prior to accommodations being approved.

LEARNING SKILLS CENTER (A1300)

Students must present their Kishwaukee College student ID when using any Learning Skills Center services. For more information on the Learning Skills Center go to http://www.kishwaukeecollege.edu/go/lsc. Tutoring is available to all Kishwaukee students free of charge.  The Writing Center (Learning Skills Center, A1306) answers your writing-related questions regardless of the class or assignment.  Students are expected to bring all material related to the assignment, including textbooks, paper prompts, etc.

Make-up tests, online tests, and placement tests are available through Testing Services, also located in the Learning Skills Center

EMERGENCY PROCEDURES/SAFETY

Yellow and red Emergency Information flipcharts are located in each classroom.  These are quick reference sheets with telephone numbers to reach emergency assistance and a brief description of the correct actions to take in the event of a tornado, fire or other emergency on campus.

RELIGIOUS OBSERVANCES

Students faced with schedule conflicts related to a religious observance should make prior arrangements with the instructor a minimum of seven (7) school days in advance of the examination or other activity involved.

STUDENT E-MAIL

Your Kishwaukee College e-mail account will be the only way to receive official notices from the College.  If you choose to forward your e-mail to another account, please be advised that all communication from and within the college will use your Kishwaukee student e-mail.  When communicating with instructors or employees of the college, you are required to use your

COMMUNITY RESOURCES

There are numerous community resources that are available to assist students in addressing a

Variety of personal needs. A listing and description of community resources can be found at

http://www.kishwaukeecollege.edu/go/communityresources

| Week | Course Schedule |  |
| --- | --- | --- |
| Week #1 | # 1. 1G – 3/8 ms plate . v –groove with backing, E7018. Introduction to Welding, Safety in Welding |  |
| Week #1 | # 1. 1G – 3/8 ms plate . v –groove with backing, E7018. Advanced shielded Metal arc wleding | #1 Due |
| Week #2 | # 2. 1G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. welding codes, standards, and coats |  |
| Week #2 | # 2. 1G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. Flame cutting | #2 Due |
| Week #3 | # 3. 2G– 3/8 ms plate . v –groove with backing, E7018. |  |
| Week #3 | # 3. 2G – 3/8 ms plate. v –groove with backing, E7018. shielded metal arc equipment setup, and operation | #3 Due |
| Week #4 | # 4. 2G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. Welder Certification |  |
| Week #4 | # 4. 2G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. weldability of metals | #4 Due |
| Week #5 | # 5. 3G– 3/8 ms plate . v –groove with backing, E7018. |  |
| Week #5 | # 5. 3G– 3/8 ms plate . v –groove with backing, E7018. Testing and Inspection of Welds | #5 Due |
| Week #6 | # 6. 3G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. |  |
| Week #6 | # 6. 3G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. Filler Metal Selection | #6Due |
| Week #7 | # 7. 4G– 3/8 ms plate . v –groove with backing, E7018. |  |
| Week #7 | # 7. 4G– 3/8 ms plate . v –groove with backing, E7018. Welding joint design, welding symbols, and fabricaton | #7 Due |
| Week #8 | # 8. 3G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. |  |
| Week #8 | # 8. 3G – 3/8 ms plate . Open v –groove. E6010 Root, E7018 fill and cover. | #8 Due |

TENTATIVE COURSE OUTLINE

Chapters to be covered  (held accountable for tests):

2 - Safety in Welding

6 - Advanced Shielded Metal Arc Welding

7 - Flame Cutting

3 - Shielded Metal Arc equipment, Setup, and Operation

19 - Welding Codes, Standards, and Costs

20 - Testing and Inspection of Welds

21 - Welder Certification

Chapters that will be referenced/overviewed (Detailed information will be specified)

1 -  Introduction to Welding

18 - Welding Joint Design, Welding Symbols, and Fabrication

24 - Weldability of Metals

25 - Filler Metal Select

Course outline is subject to change.

Welding Coupon Sheet attachment as follows.

NOTE:

Any major course revision in the outline, grading system, or course requirements must have prior approval of the Division Dean and be provided in writing to ALL students with copies to the Division Office.

Language on the syllabi course materials developed by INAM funds:

From the grant agreement’s Part IV  Special Conditions, Item 15, Intellectual Property Rights, the following needs to be on all products developed in whole or in part with grant funds:

“This workforce solution was funded by a grant awarded by the U.S. Department of Labor’s Employment and Training Administration. The solution was created by the grantee and does not necessarily reflect the official position of the U.S. Department of Labor. The Department of Labor makes no guarantees, warranties, or assurances of any kind, express or implied, with respect to such information, including any information on linked sites and including, but not limited to, accuracy of the information or its completeness, timelines, usefulness, adequacy, continued availability, or ownership. This solution is copyrighted by the institution that created it. Internal use, by an organization and/or personal use by an individual for  non-commercial purposes, is permissible. All other uses require the prior authorization of the copyright holder.”

| Kishwaukee Community College Name Class SMAW II WT 124 Semester Spring 2014 | Weld Size | Weld Consistency | Weld Contour | Surface Irregularities | Undercut | Cold Lap | Overlap | Reinforcement | Bead Sequence Tie-in | Restart | Slag | Spatter | Porosity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| grade | # | type | process | joint | filler |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Mid –Term | Theory | NA | NA |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | Final | Theory | NA | NA |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 1 | 1G | SMAW | V-Groove/backing | E7018 |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 2 | 1G | SMAW | V-Groove Open root | E6010Rt E7018Fill |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 3 | 2G | SMAW | V-Groove/backing | E7018 |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 4 | 2G | SMAW | Open Root | E6010Rt E7018Fill |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 5 | 3G | SMAW | V-Groove/backing | E7018 |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 6 | 3G | SMAW | Open Root | E6010Rt E7018Fill |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 7 | 4G | SMAW | V-Groove/backing | E7018 |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 8 | 4G | SMAW | Open Root | E6010Rt E7018Fill |  |  |  |  |  |  |  |  |  |  |  |  |  |
| EC | 9 | 1G | SMAW | Open Butt | 6010R 7018B |  |  |  |  |  |  |  |  |  |  |  |  |  |
| EC | 10 | 2G | SMAW | Open Butt | 6010R 7018B |  |  |  |  |  |  |  |  |  |  |  |  |  |
| EC | 11 | 3G | SMAW | Open Butt | 6010R 7018B |  |  |  |  |  |  |  |  |  |  |  |  |  |
| EC | 12 | 4G | SMAW | Open Butt | 6010R 7018B |  |  |  |  |  |  |  |  |  |  |  |  |  |

COMMENTS:  X = Excellent  (blank) = Good    √ = Average   / = Needs Improvement    -  =  Insufficient   + =Excessive

7-31-13sl